## Slide 1
Unit Tutor: Dr. Roodheer BEEHARRY
Unit 6 –Engineering Properties & Applications of Polymeric Materials
Metallic and Polymeric Materials for Civil Engineering
Civil & Environmental Engineering Department

## Slide 2: Content
Applications of Polymers in Building & Civil Infrastructure
Salient features of Polymers
Classification of Polymers
Polymer configurations – Linear, Branched or Cross-linked
Homopolymer or Copolymer
Chain Isomerism in polymers
Thermoplastics & Thermosets
Crystallinity in polymers
Fibres, Plastics and Elastomers
Polymerization mechanisms
Thermomechanical behaviour of polymers
Factors influencing Tg
Mechanical properties of polymers
Factors that Influence Mechanical Properties
Polymer degradation
Improvement of Polymer Properties

## Slide 3: Applications of Polymers in Building & Civil Infrastructure
Polymers have become essential as an engineering construction material;
Geosynthetics; geotextiles, geomembranes, geopipes, geofoams, geogrids, geocells, geonets, geocomposites and geosynthetic clay liners. Common geosynthetic polymers are PE, PP, PVC, PET, PA, PS and CSPE.
Bridge bearings; Neoprene pads deflects in shear to accommodate expansion, contraction, and end rotation of the bridge structure.
Piping and Conduit; large diameter pipes for sewage, drainage and potable water, cabling, rainwater collection, etc
Coatings; protect surfaces prevent the corrosion of metals, floorings.
Adhesives and sealants; the basis of all engineering adhesives & sealants.
Concrete-polymer hybrids; Polymer-impregnated and polymer concrete.
Seals and Gaskets; aperture seals, gaskets and expansion joints.
Cladding and profiles; for windows, doors, coving, and skirting.
Insulation; panels or sandwiched into construction of walls and roofs.
Polymer composites; Fibre-reinforced concrete & Fibre reinforced polymer

## Slide 4: Salient features of Polymers
Polymeric materials offer high stiffness-to-weight ratios, durability, electrical insulation/conduction and which often results in reduced costs.
Polymers consist of long, chain-like molecules built of covalently bonded thousands of repeating chemical units (monomers or mers), contain 103 to 106 atoms and have molecular weights ranging from about 103 to 105.
Transformation of mer molecules to a polymer is known as polymerization.
Prior to polymerization most polymers exist as low-viscosity fluids known as oligomers typically containing perhaps 1-10 mers.
The functionality of a mer equals the number of covalent bonds the mer can form with other chemical groups. If it can form two bonds, it is a difunctional mer. A monofunctional mer can form only one covalent bond, and therefore cannot exist as the repeat unit in a polymer. Trifunctional or tetrafunctional mers can form three or four covalent bonds, respectively.
Mers are generally simple organic molecules containing a double bond or a minimum of two active functional groups. The number of mers in a polymer chain is called the degree of polymerization.

## Slide 5: Classification of Polymers
Polymer can be classified based on different basis, namely;
Origin – Natural, Synthetic, Semi-synthetic.
Line structure – Linear, Branched, Cross-Linked, Networked.
Thermal response – Thermoplastic and Thermoset
Mode of Formation – Addition, Condensation
Crystallinity – Amorphous (non-crystalline), Semi-crystalline, Crystalline
Application – Plastics, Elastomers (Rubbers), Fibres
Tacticity – Isotactic, Syndiotactic, Atactic
Chain – Co- or Homo- & Polarity – Polar, Non polar
Natural polymers - made from natural materials like plant and animal products; ex. cellulose, collagen, starches, hair, fingernails, tar, crab shells, DNA/RNA)
Synthetic polymers are made from petrochemicals, like oil and natural gas.
Semi-synthetic polymers are made from a combination of natural and synthetic materials.

## Slide 6: Polymer configurations – Linear, Branched or Cross-linked
The functionality of a molecule is simply its interlinking capacity, or the number of sites it has available for bonding with other molecules under the specific polymerization conditions. Affects Ability to Crystallize
Linear - Bifunctional structural units can enter into only two linkages with other structural units. This means that the sequence of linkages between bifunctional units is necessarily linear, resulting in a linear polymer.
Branched - The reaction between polyfunctional molecules results in structural units that may be linked so as to form nonlinear structures. In some cases the side growth of each polymer chain may be terminated before the chain has a chance to link up with another chain. The resulting polymer molecules are said to be branched.
Cross-linked – In other cases, growing polymer chains become chemically linked to each other, resulting in a cross-linked three-dimensional molecular network system. A ladder polymer consists of two parallel linear strands of molecules with a regular sequence of crosslinks.
Heavily cross-linked polymer chains are also called network polymers.

## Slide 7: Homopolymer or Copolymer
Polymers composed of only one repeating unit in the polymer molecules are known as homopolymers.
Polymers composed of two different repeating units in the polymer molecule are defined as copolymers.
Depending on arrangement along the backbone and the possibility for one type of backbone to have branches of another type, we can have;
Random copolymer — the repeating units are arranged randomly on the chain molecule (ex. AABBABABBAAABAABBA)
Alternating copolymer — there is an ordered (alternating) arrangement of the two repeating units along the polymer chain (ex. ABABABABAB)
Block copolymer — the chain consists of relatively long sequences (blocks) of each repeating unit chemically bound together: (AAABBBBBAAAAAABB).
Graft copolymer — Sequences of one monomer (repeating unit) are ―grafted onto the backbone of the another monomer type.

## Slide 8: Chain Isomerism in polymers
Isomerism; same chemical formula but different chemical structure. Polymer molecules have many conformations and might have different configurations. Conformations concerns rotation about the backbone, while configurations is concerned with bonds.
Positional isomerism: have the same molecular formula, but different connectivities. Example head-to-head, tail-to-tail, head-to-tail
Geometrical isomerism – Configurations (cis and trans) describe the arrangements of identical groups of atoms around a double bond in a repeat unit, rotation around the double bond is restricted. The functional group is placed differently (same side or not) with regards to the double bond. The properties of the cis- and trans-isomers can be quite different.
Stereoisomerism (Tacticity): The difference in configuration due to the orientation of different functional groups with respect to the main chain. There are 3 ways in which the position of the pendant side group can exist, for example, it can occur all on one side (isotactic), on alternate sides (syndiotactic) or placed at random (atactic).

## Slide 9: Thermoplastics & Thermosets
Thermoplastics - These polymers on heating become soft and on cooling again become hard and retain their original shape. In this case, the intermolecular forces, on heating weakens and the polymer becomes soft and vice-versa. It is purely a physical change and physical changes are generally reversible. Therefore, these polymers are recyclable, i.e., they can be moulded and re-moulded again and again, and can be amorphous or crystalline. e.g. PE, PP, PVC, PVAC, PS, PC, PMMA, SAN, ABS, POM, CA, etc.
Thermosets - Although they might be heated to the point where they would soften and could be made to flow under stress once, but would not do so reversibly. Heating caused them to undergo a “curing” reaction. Further heating of these thermosetting polymers ultimately leads only to degradation. In this case, the cross links get broken and rearranged on heating. It is purely a chemical change and chemical changes are generally irreversible. Therefore, these polymers are not recyclable, i.e., once moulded, they cannot be moulded again. These polymers greatly improve the material’s mechanical properties. e.g., epoxies, silicones, UPE, PF, MF, UF, PUR, etc.

## Slide 10: Crystallinity in polymers
Crystalline polymers are in fact semi-crystalline because there are always some amorphous regions, depending upon factors such as the shape of their repeat unit, their molecular weight and their thermal history. Crystallinity in polymers is more complex because of the long polymer chains. In some areas, the polymer chains align and pack together to form crystals; in other areas, the chains are disordered and cannot pack together, so semi-crystalline polymers tend to have crystalline regions dispersed within amorphous material. The degree of crystallinity may vary from a few percentage to about 90% depending on the crystallization conditions.
E.g. of crystalline polymers include polyethylene, polyacrylonitrile, poly (ethylene terephthalate), and polytetrafluoroethylene.
Amorphous Polymers | Semi-crystalline Polymers
Softens with increasing temperature | Almost well-defined melting point
Good formability | Poor formability
High transparency | Opaque
Poor chemical resistance | Good chemical resistance
Bonds well using adhesives | Difficult to bond with adhesives
Poor fatigue resistance | Good fatigue resistance
Poor wear resistance | Good wear resistance

## Slide 11: Fibres, Plastics and Elastomers
In primary valence bonding, atoms are tied together to form molecules using their valence electrons. This generally leads to strong bonds.
Secondary bonds (Van der Waals, Hydrogen, and Dipole bonds), do not involve valence electrons and are relatively weak. Molecules must come together as closely as possible for secondary bonds to have maximum effect.
Fibres are linear polymers with close alignment of molecules, high symmetry and high intermolecular forces. They have high modulus and tensile strength and, moderate extensibilities (usually < 20%).
Elastomers have irregular structure, weak intermolecular attractive forces, a few cross-links and have very flexible polymer chains. Have high extensibility (up to 1000%) and recover rapidly on the removal of the imposed stress, have low initial modulus, but stiffen when stretched.
Plastics are between the structural extremes of fibres and elastomers. The demarcation between fibres and plastics may sometimes be blurred. PP and PA can be used as fibres or as plastics by the proper choice of processing.

## Slide 12: Polymerization mechanisms (I)
There are four types of polymerisation reactions; (i) Addition or chain growth polymerisation, (ii) Coordination polymerisation, (iii) Condensation or step growth polymerisation and (iv) Copolymerization.
Addition Polymerisation; it is simply the addition of monomer molecules (same or different) of unsaturated compounds to each other without loss of any atoms from the original monomer molecules. It is a chain reaction consisting of 3 stages, namely; Initiation, Propagation and Termination.
Initiation stage; an initiator molecule reacts to generate an "active species“ (a cation, or an anion, or a free radical) which then initiates the polymerization by adding to the monomer's carbon=carbon double bond.
Propagation stage; The initial monomer with newly generated "active species" becomes the first repeat unit in the incipient polymer chain and adds to another monomer. This procedure is repeated over and over.
Termination stage; the growing chain terminates through reaction with, another growing chain or with another species or by decomposition.

## Slide 13: Polymerization mechanisms (II)
Coordination polymerization; is a subclass of addition polymerization. The "active species" is a coordination complex, which initiates the addition polymerization involving carbon=carbon double bond. The most important catalyst for coordination polymerization is the Ziegler-Natta catalyst which combine transition metals with organometallic compounds.
Condensation Polymerisation or Step-growth; involves a repetitive condensation reaction (2 molecules join with loss of small molecules such as water, alcohol, etc.) and the sequence of condensation goes on. Monomers with only one reactive group terminate a growing chain, and thus give end products with a lower molecular weight. Linear polymers are created using monomers with two reactive end groups and monomers with more than two end groups give three dimensional polymers which are cross linked.
Copolymerization; is a reaction in which a mixture of more than one monomer species is made to polymerize and form a copolymer. The copolymer can be made not only by chain growth polymerisation but by step growth polymerisation too.

## Slide 14: Thermomechanical behaviour of polymers
Polymers have a range of mechanical behaviour which are highly temp.-dependent, the variation near room temperature is important.
The mechanical behaviour vary from brittle-elastic at low temperatures, through plastic to viscoelastic or leathery, to rubbery and finally to viscous at higher temperatures (relatively small variation -20°C to +200°C)
Glass transition temperature (Tg);It’s the temperature at which an amorphous polymer material turns into a rubbery form when heated.
At Tg, the main backbone chain mobility changes. At lower temperatures there is still molecular motion but the main backbone chain is frozen in place.
Tg for a given plastic can be changed by
incorporation of a plasticizer. Pure crystalline
polymers do not have a glass transition temperature.
Pure amorphous polymers do not have a melting
temperature. Most polymers have both a glass
transition temperature and a melting temperature.
.

## Slide 15: Factors influencing Tg
Molecules are virtually frozen in position below Tg begin to experience rotational and translational motions above Tg.
Knowledge of Tg allows an immediate assessment of the general nature of the polymer at room temperature. A polymer with a very low Tg is "rubbery" and ductile at room temperatures, whereas a polymer with a very high Tg is "glassy" or "rigid" and brittle at room temperatures.
Higher molecular weight (Mw) tends to increase Tg.
Presence of bulky side groups increase chain stiffness and increase Tg.
Polar side atoms or groups of atoms stiffen chain and increase Tg.
Double=chain bonds or aromatic chain groups stiffen the molecular backbone and increase Tg.
A small amount of branching will tend to lower Tg; on the other hand a high density of branches reduces chain mobility and elevates Tg.
As crystallinity increases Tg also increases.
As cross linking increases Tg also increases.
Addition of plasticizer decreases Tg.

## Slide 16: Mechanical properties of polymers
Mechanical properties; denoted by stress-strain curve, depend on temperature, time and frequency of loading.
Tensile strength (TS) often increases with Mw.
TS and E often increase with % crystallinity.
- brittle response (aligned, cross-linked, networked)
- plastic response (semi-crystalline case)
For plastics , yield strength is defined by the
maximum on curve just after the elastic region.
- Plastic deformation is defined by the interaction between crystalline and
amorphous regions and is partially reversible.
Tensile strength - defined at the fracture point and can be < yield strength.
Mechanical properties of polymers change acutely with temp., from glass-like brittle behaviour at low temp. to a rubber-like behaviour at high temp.
Stress decreases with time due to molecular relaxation processes.
Many polymers susceptible to time-dependent deformation under constant load – viscoelastic creep.

## Slide 17: Factors that Influence Mechanical Properties
Temperature and strain rate (time)
Chain entanglement, strong intermolecular bonding (van der Waals, cross-links) increase strength
Drawing, analogue of work hardening in metals, corresponds to the neck extension. Is used in production of fibres and films. Molecular chains become highly oriented ⇒ properties of drawn material are anisotropic (perpendicular to the chain alignment direction strength is reduced)
Heat treatment - changes in crystallite size and order
- undrawn material: Increasing annealing temperature leads to;
increase in elastic modulus
increase in yield/tensile strength
decrease in ductility
Note that these changes are opposite to those of metals
- drawn material: opposite changes (due to recrystallization and loss of
chain orientation).

## Slide 18: Polymer degradation
Oxidative degradation - an autocatalytic process of attack on the hydrogen atoms, to form hydroperoxides. Appropriate stabilizers need to be used.
Radiation degradation - UV wavelengths selectively excite electrons in the polymer chain. This increases the vibrational and rotational energy of the covalent bonds, leading to degradation by bond cleavage. Degradations include yellowing, chalking, surface embrittlement, loss of tensile or impact strength, and cracking. Pigments such as carbon black are commonly added to absorb ultraviolet radiation and then re-emit it as thermal energy.
Microbiological degradation – Low Mw hydrocarbons (low density PE) can be degraded by microbes.
Chemical attack - Organic liquids, such as cleaning fluids, detergents, petrol and lubricants may seriously reduce the mechanical properties of plastics. It’s most serious when a material is exposed to aggressive fluids when it is under stress. Chemical interactions may involve a decrease in Mw by chain breakage; this may cause a reduction in mechanical properties such as tensile strength, stiffness and fracture toughness. Absorbed moisture can act as a plasticizer, reducing Tg and the strength of the polymer.

## Slide 19: Improvement of Polymer Properties
Polymer Additives - Improve mechanical prop, processability, durability ,etc.
Fillers – Added to improve tensile strength & abrasion resistance, toughness & decrease cost. E.g. carbon black, silica gel, wood flour, glass, limestone, talc, etc (size 10nm)
Plasticizers (liquids, low vapour pressure, low Mw)
– Added to reduce the glass transition temperature Tg
– commonly added to PVC - otherwise it is brittle
Stabilizers (counteract deterioration, increase mechanical integrity)
– Antioxidants (consume O2 before it reaches polymer or block reaction)
– UV protectants (thin adsorbent layer: sunscreen; material that react with
bonds broken by UV)
Flame Retardants - reduce the inherent flame risk of polymer substrates by lowering the rate of flame spread under fire conditions.
Lubricants – Added to allow easier processing.
Colorants – Dyes (dissolved in polymer) or pigments (separate phase)

## Slide 20: THANK YOU