## Slide 1
Unit Tutor: Dr. Roodheer BEEHARRY
Unit 7 – Polymer Based Composites & Emerging Materials for Civil Engineering
Metallic and Polymeric Materials for Civil Engineering
Civil & Environmental Engineering Department

## Slide 2: Content
Characteristics of Composite Materials
Classification of Composite Materials
Particle-Reinforced Composites
Polymer Concretes
Fibre-Reinforced Concretes (FRCs)
Fibres for Fibre-Reinforced Composites
Matrices for Polymer-Matrix Composites
Functional Requirements for Fibres & Matrix
Fibre-Matrix Interface
Fabrication of FRP Composites
Mechanical Properties of FRP Composites
Advantages of FRP over traditional materials
Limitations of FRP over traditional materials
Applications of FRPs in the Civil Engineering sector
FRPs - Emerging Materials for Civil Engineering

## Slide 3: Characteristics of Composite Materials
A typical composite material is a system of materials composing of two or more materials (mixed and bonded) on a macroscopic scale.
Composites consist of one or more discontinuous phases embedded in a continuous phase. The discontinuous phase is usually harder and stronger than the continuous phase and is called the ‘reinforcement‘ or ‘reinforcing material’, whereas the continuous phase is termed as the ‘ matrix’.
The reinforcement (fibres, particles, flakes, and/or fillers) is embedded in the matrix (polymers, metals, or ceramics) which holds the reinforcement to form the desired shape while the reinforcement improves the overall mechanical properties of the matrix. Designed properly, the new combined material exhibits better strength than would each individual material.
The nature of the constituent materials, the geometry of the reinforcement (shape, size and size distribution) influences the properties of the composite to a great extent. The concentration, distribution and orientation of the reinforcement also affect the properties.
Two broad classes :Fibrous composites & Particulate composites

## Slide 4: Classification of Composite Materials
A composite material is a multiphase material, a mixture or combination of two or more micro or macro-constituents (matrix and reinforcement) that differ in form and composition and do not form a solution.
The Matrix phase (continuous): continuous part that surrounds the other phase. It transmit and distribute external stresses to the dispersed phase and protect the latter from the environment.
Matrix-based classification: Metal Matrix Composites (MMC), Ceramic Matrix Composites (CMC) & Polymer Matrix Composites (PMC)
The Reinforcement (discontinuous or dispersed phase): stiffer, high strength part, it enhances matrix properties.
Reinforcement-based classification:
Particle-reinforced; can be large particles or dispersion-strengthened (<10nm)
Fibre-reinforced; can be continuous aligned or short discontinuous (aligned or randomly oriented)
Structural; can be laminates or sandwich panels.

## Slide 5: Particle-Reinforced Composites
Concrete (an ancient composite) – composite material on many levels. At the macroscopic level concrete consists of coarse aggregate embedded in a cement matrix; on a finer scale the mortar itself consists of sand embedded in a matrix of hydrated cement paste. On a microscopic level, the hydrated cement contains a network of crystallized particles, grains of unhydrated cement in a system of gel.
Reinforced concrete – adding reinforcement bars or wire mesh to the concrete to improve/ increase its tensile strength and reduce cracking.
Prestressed concrete;
- Rebar/wire-mesh (grid) placed under tension during setting of concrete
- Release of tension after setting places concrete in a state of compression
- To fracture concrete, applied tensile stress must exceed this compressive stress.
- Posttensioning – tighten nuts to place hardened concrete under compression

## Slide 6: Polymer Concretes
Polymer concrete mixes are very common as concrete patching materials, impermeable toppings over bridge decks, grout for installing tile, additives for plaster, stucco and EIFS.
Polymer Impregnated Concrete (PIC); ordinary concrete is cured and dried in the oven, then air is removed from it by vacuum in an open cell. Polymerization is done by radiation or heat, using a low viscosity monomer.
Polymer-modified concrete; so-called when polymers are added to the concrete. There are several benefits of using polymer-modified concrete, namely: Increased strength and durability; Improved workability (use of latex admixtures); Lower water permeability; Increased freeze-thaw stability; Better resistance to chemicals
Polymer Cement Concrete (PCC): is prepared from a mixture of cement, aggregate, water, and monomer. The mixture is cast in place then cured, dry, and polymerized.
Polymer Concrete (Resin Concrete): Polymer is used instead of cement as the binder in concrete. Polymer or Monomer is mixed with dry aggregate and cast in place. It hardens through polymerization.

## Slide 7: Fibre-Reinforced Concretes (FRCs)
Short fibres used in concrete can be characterized in different ways according to the fibre material: natural organic (cellulose, sisal, jute, bamboo, etc.); natural mineral (such as asbestos and rock-wool); or man-made (e.g. steel, titanium, glass, carbon, polymers or synthetic)
Synthetic fibres that have been used in Portland-cement-concrete based matrices include: acrylic, aramid, carbon, nylon, polyester, polyethylene, Polyvinyl alcohol fibres (PVA) and polypropylene.
Fibres are usually used in concrete to control plastic shrinkage cracking and drying shrinkage cracking. They also lower the permeability of concrete and thus reduce bleeding. Some types of fibres can improve impact, abrasion and shatter resistance in concrete.
Applications include overlays and over slabbing for roads, pavements of air fields, bridge decks, industrial and other flooring subjected to wear and tear and chemical attack.
Polymer fibres; beneficial in corrosive environment or structures submerged in water such as bridges and dams.

## Slide 8: Fibres for Fibre-Reinforced Composites
Glass fibre is the oldest and very common as reinforcement in composites. Binders and coatings (lubricants) are required for fiberglass products.
Carbon fibre, its E-value ranges from regular to ultra-high modulus and provides exceptionally high properties in both tension & compression.
Aramid fibre have one of the highest strength to weight ratio compared to other fibres. Its properties depend on the manufacturing process.
Basalt fibre has a high melting point, allowing it to be exposed to high temperatures for extended periods of time and is highly anti-corrosive.
Boron fibre is five times as strong and twice as stiff as steel, has excellent compressive properties and buckling resistance.
Polypropylene fibre extremely light weight, excellent chemical and moisture resistance, outstanding impact resistance, antiballistic properties.
Polyester fibre is fairly low weight and has improved toughness & stiffness.
Hybrid fibres such as Aramid/Glass, Carbon/Polypropylene, Basalt/ Polypropylene and Glass/ Polypropylene

## Slide 9: Matrices for Polymer-Matrix Composites
Matrices for the production of polymer-matrix composites include a variety of thermoplastics and thermosets
Thermoplastics; both amorphous and crystalline thermoplastics are used in the production of high performance composites.
PEEK, is a semi-crystalline aromatic polymer and many of its properties depend on the degree of crystallinity.
Other crystalline aromatic TPs used as a composite matrix include aromatic polyamides, aromatic polyesters, polyphenylene sulphide (PPS), polyphenylene oxide (PPO) and polyimide.
Thermosetting resins such as polyesters and phenolics are used with glass fibre in producing economic-grade glass-fibre reinforced plastics (GRP).
Epoxy resins and polyimides are employed with fibres such as carbon fibre and Kevlar in the manufacture of high-performance composites.
Other TSs include aminoresins mainly Urea-formaldehyde (UF) & Melamine formaldehyde (MF), Vinyl ester resins and Bismaleimides.

## Slide 10: Functional Requirements for Fibres & Matrix
Requirements for Fibres; - Uniform diameter
- High modulus of elasticity to give stiffness
- High ultimate strength
- Low variation of strength between individual fibres
- Stability during handling
Requirements for Matrices;
Wet out the fibre and cure satisfactory in the required conditions
Bind together the fibres and protect their surface from abrasion and environmental ageing
Disperse the fibres and separate them in order to avoid any catastrophic propagation of cracks
Transfer stresses to the fibres efficiently
Be chemically and thermally compatible with fibres
Have appropriate fire resistance and limit smoke propagation
Provide good aesthetic finish (colour and surface).

## Slide 11: Fibre-Matrix Interface
The fibre-matrix interface is where the very important function of load transfer from matrix to the fibres occurs and, therefore, it has a major influence on the properties of composite materials. The strength of adhesion between the fibres and matrix depends on;
Molecular entanglement (interdiffusion):
- Entanglement of molecules at the interface.
- Especially important in fibres that are precoated with polymers.
- Molecular conformation/structural and chemical aspects.
Electrostatic attraction - depends on surface charge density (e.g. glass fibres, polymers groups with charges.
Covalent bonding
- Usually the strongest fibre matrix fibre-interaction.
- The most important in many composites.
Mechanical adhesion
- Interlocking of 2 rough surfaces (e.g. thermosetting resins)

## Slide 12: Fabrication of FRP Composites
Pultrusion - Tightly packed tows of fibres, impregnated with polymer, are pulled through a shaped heated die to form aligned, continuous sections such as reinforcing bars and tendons, I-beams and hollow sections.
Filament winding - involves winding fibres over a mandrel which rotates while a moving carriage lay down the reinforcement in the desired pattern.
Compression and Transfer Moulding -shape resins with short glass fibres.
Matched-die moulding and autoclave - laminates and retrofit sheets.
Continuous sheet production - Chopped strand mat or chopped strands are impregnated with resin and sandwiched between two layers of film on a moving belt to form corrugated or other desired profile.
Resin transfer moulding and vacuum assisted resin transfer moulding - produce claddings, roofing panels, shell structures and bridge decks.
Contact moulding by hand lay-up or spray-up - Open mould methods, where fibre continuous strand mat and/or other fabrics such as woven roving are placed manually in the mould and each ply is impregnated with brushes and rollers.

## Slide 13: Mechanical Properties of FRP Composites
The mechanical properties of FRPs depend on a number of factors:
- The relative proportions of fibre and matrix.
- The mechanical properties of the constituent materials.
- The orientation of the fibre within the matrix.
- The method of manufacture.
The Young’s modulus and tensile strength of composites are lower than that of fibres alone. Elastic modulus Glass fibres < Carbon fibres.
Regardless of the type of fibres employed, FRP materials have similar stress-strain behaviour: linear elastic up to final brittle rupture when subject to tension, they do not possess the ductility that steels have.
This brittleness limit the ductile behaviour of RC members strengthened with FRP composites. When used to provide confinement for concrete, these materials can greatly enhance the strength and ductility of columns.
FRPs have ultimate strengths that can be many times greater than steel.
Both glass and aramid FRPs have moduli that are considerably less than steel, but carbon FRPs have moduli that are lower but comparable to steel.

## Slide 14: Advantages of FRP over traditional materials
High Specific Strength and Stiffness; Fibre reinforced composites have high strength-to-weight and stiffness-to-weight ratios.
Corrosion resistance; FRPs possess a substantially higher resistance to corrosion, aggressive media and chemical reagents, making them attractive in application where corrosion is a concern. This allows long service life without additional maintenance costs.
Enhanced Fatigue Resistance; Most composites are considered to be highly resistant to fatigue to the extent that it can be neglected at the materials level in a number of structures, leading to design flexibility.
Rapid construction; FRPs can be fabricated off-site and shipped to the construction site easily and installed using light equipment.
Dimensional stability & Aesthetics; prefabrication and assembly ensure dimensional accuracy. Pigments can be used to improve colour.
Resistance to frost and de-icing salt; FRPs composites show good resistance during freeze-thaw cycles and are resistant to de-icing salts.

## Slide 15: Limitations of FRP over traditional materials
Higher short-term and uncertain long-term costs; material and fabrication costs of FRP composites for civil engineering are still high compared to traditional materials. Long-term cost are still under study.
Uncertain durability; the standardization of lab tests and the calibration based on real environmental conditions still under study.
Lack of ductility; FRP composites do not show definite yield like steels.
Low fire resistance; FRPs have low fire resistance. Fire-retardant & self-extinguishing types exist but loss of strength in fire is still studied.
Lack of Design Standards; mostly design guides available.
Lack of Knowledge on Connections; the design of connections in FRP composite structural systems is still not well developed.
Surface Preparation and Bonding of FRP; Structural strengthening is done on site, surface treatment must adequate and easily done under field conditions which is key to a strong, effective and durable bond.

## Slide 16: Applications of FRPs in the Civil Engineering sector
Commonly used FRPs in civil engineering include carbon FRPs (CFRP), glass FRPs (GFRP), aramid FRPs (AFRP), and basalts FRP (BFRP).
FRP bars, rods and grids; the use of FRP reinforcing bars and grids for concrete is a growing segment of the application in structural engineering.
FRP cables for prestressing and post-stressing; used in the construction of suspension and stay cables for bridges, pre-stressed tendons, etc.
Repair and Strengthening for structural rehabilitation; Repair with FRP composites has been used successfully on concrete (bridges), timber, metal and masonry structures.
Seismic Retrofit; for structurally deficient RC structures in seismic regions. It provides a means of confinement, without increasing the stiffness and also enables the rapid fabrication of cost effective and durable jackets.
New FRP Civil Structures; include compound curved roofs, bridges decks, energy absorbing roadside guardrails, building systems, rooftop cooling towers, offshore platforms, marine structures such as seawalls and fenders.

## Slide 17: FRPs - Emerging Materials for Civil Engineering
FRP - widely used, in many European and North American countries for strengthening structures, repair of building, bridges and new structures.
Looking at the trend it is clear that the volume of repair and retrofit works with FRPs will increase substantially in the future.
If appropriately designed and fabricated, FRPs can grant longer lifetimes and lower maintenance costs than equivalent structures fabricated from conventional materials
Recent advances in smart materials and smart structures, FRP materials have been developed which include fibre-optic sensors (FOS) as part of their internal structure which can be used to measure internal variations in strain and temperature, and monitor the short- and long-term behaviour and performance of the built infrastructure.
Current research is focused on improving composites by using fibres roughly 1000 times smaller (nanocomposites) which use carbon nanotubes or nanoparticles as the reinforcement and are likely to be cheaper & have better mechanical properties than traditional composites
.

## Slide 18: THANK YOU