## Slide 1
Unit Tutor: Dr. Roodheer BEEHARRY
Unit 5 –Welding processes & Weldability of Steels
Metallic and Polymeric Materials for Civil Engineering
Civil & Environmental Engineering Department

## Slide 2: Content
How Does Welding Work?
Classification of Welding processes
Effect of Atmospheric Air on Welding
Electric Arc Welding Processes
Shielded Metal Arc Welding (SMAW)
Heat flow in welding
Effect of the Welding Thermal Cycle on the Microstructure
The Heat Affected Zone (HAZ)
Vulnerabilities of the Heat Affected Zone (HAZ)
Residual Stresses and Distortion in Welding
Residual Stress Relief
Weld Metal Solidification Cracking
Weldability of Steels
Types of Weld Defects
Quality Criteria in Welding
Inspection and testing of Welds
Laser Beam welding

## Slide 3: How Does Welding Work?
The 3 main components needed to create a weld are:
A heat source such as an electric arc or a flame. The most common heat source is an electric arc. An arc is the physical gap between the end of the electrode and the base metal. The physical gap causes heat due to resistance of current flow and arc rays. The arc melts the metals.
Shielding - a substance used to protect the weld from air as the weld is being formed. Oxygen from the air makes welds brittle and porous. In arc welding, a flux or a non-reactive (inert) gas is used to 'blanket' the weld pool and thus exclude air.
Filler material, which is the material used to join to the two pieces together.
Fusion welding without pressure - A method of welding in which similar and dissimilar metals are joined together by melting their joining edges with or without the addition of filler metal but without applying pressure.
Fusion welding with pressure - similar metals are joined together by heating them to plastic or partially molten state and then joined by pressing without the use of filler metal.

## Slide 4: Classification of Welding processes (I)
Welding offers a means of making continuous, load bearing, metallic joints between the components of a structure. There are many welding processes. The type of welding process used is related to the specific task.
According to the sources of heat, welding processes can be classified as:
- Electric welding processes (heat source is electricity)
- Gas welding processes (heat source is gas flame)
- Other welding processes (heat source is neither electricity nor gas flame)
Electric welding processes can be classified as:
- Electric arc welding
- Electric resistance welding
- Laser welding
- Electron beam welding
- Induction welding

## Slide 5: Classification of Welding processes (II)
Electric arc welding can be further classified as:
- Shielded Metal Arc Welding (SMAW) or Manual Metal Arc Welding (MMAW)
- Carbon arc welding
- Atomic hydrogen arc welding
- Gas Tungsten Arc Welding (GTAW) or Tungsten Inert Gas (TIG) Welding.
- CO2 gas arc welding
- Flux core arc welding
- Submerged arc welding
- Electro-slag welding
- Plasma arc welding
Resistance or pressure welding uses the application of pressure and current between two metal surfaces to create fusion:
- Spot welding
- Seam welding
- Laser welding, - Flash butt welding and, - Projection welding.

## Slide 6: Classification of Welding processes (III)
Gas welding processes can be classified as:
- Oxy-acetylene gas welding
- Oxy-hydrogen gas welding
- Oxy-coal gas welding
- Oxy-liquefied petroleum gas welding
- Air acetylene gas welding
The other welding processes are:
- Thermit welding
- Forge welding
- Friction welding
- Ultrasonic welding
- Explosive welding
- Cold pressure welding and, - Plastic welding

## Slide 7: Effect of Atmospheric Air on Welding
Air is a gaseous mixture of mainly nitrogen and oxygen, with other minor constituents gases like hydrogen, etc.
When hot or molten iron comes in contact with air the metal gets oxidized.
Oxygen contamination (oxidation) will reduce the mechanical properties (tensile strength, toughness and ductility of the weld metal and will also;
Produce blow holes in the weld.
Produce oxides which will dissolve in the molten metal and make the metal brittle and weak.
The oxides of wrought iron and steel melt at a temperature lower than that of the parent metal, and being light, float to the surface as a scale.
If nitrogen contaminates the weld pool during the solidification of the weld
metal, it forms bubbles and results in the formation of gas porosity. Also,
atmospheric nitrogen will combine with the molten metal to form iron
nitride which causes the weld to harden.
The formation of oxides and nitrides due to the contact of atmospheric air with the molten metal is also called as atmospheric contamination.

## Slide 8: Electric Arc Welding Processes
An electric arc is formed between the terminals (air gap) of an electric circuit. It produces very intense heat in the form of a spark (app. 3600°C).
Metallic arc welding – arc is formed between a metallic (consumable) electrode (which melts itself and acts as a filler metal) and the parent metal.
Carbon arc welding - arc is formed between a carbon electrode (non-consumable) and the metal. A separate filler rod is used.
Atomic hydrogen arc welding - arc is formed between two tungsten electrodes in hydrogen gas. A separate filler rod is used.
Tungsten inert gas welding (TIG) - arc is formed between tungsten electrodes (non-consumable) and metal in an inert gas (argon or helium).
Metal inert gas arc welding (MIG or GMAW); arc is formed between a metallic consumable electrode and metal in an inert gas. If gas is CO2 , MAG.
Submerged arc welding – same as MIG except arc under a heap of powdered/ granulated flux. Arc is totally submerged in the flux and invisible
Electro-slag welding – same as MIG, arc formed under molten flux (slag).
Plasma arc welding - tungsten electrode, in plasma-forming gas; N, H &Ar.

## Slide 9: Shielded Metal Arc Welding (SMAW)
The electric arc develops when electricity jumps across an air gap (ionization of air) between the end of the metallic electrode and the metal.
The metallic electrode is generally coated with a flux which is consumable.
The arc created due to the ionization of air between the electrode tip and the base metal generates an intense arc heat having a temperature between 3600°C - 4000°C which melts a small portion of the metal directly under the arc and the end of the electrode instantaneously.
The flux coating on the electrode also melts and provides a gaseous shield around the arc which protects the molten metal from atmospheric contamination. Hence this is called shielded metal arc welding (SMAW).
The slag (from flux coating) gets deposited on the surface as it is lighter than the metal and the weld metal is allowed to cool gradually and slowly.
The welding speed and feed of the electrode is controlled manually by the welder himself. So it is also called manual metal arc welding (MMAW).

## Slide 10: Heat flow in welding
Quality welding requires maintaining the specified thermal conditions in and near weld metal within specific limits to control metallurgical structure, mechanical properties, residual stresses, and distortions that result from a welding operation.
The rate of heat input to the workpiece during welding is governed by magnitude and rate of energy input at the weld, the distribution of heat input, and the weld travel speed. Heat transfer in a weldment forms a time-dependent temperature distribution. The weld undergoes a thermal cycle that varies from location to location depending on the heat input, weldment geometry, and material properties.
When the weld pool is cooling and solidifying, the majority of the heat flows through the parent metal alongside the joint. The steel is thus subjected to heating and cooling cycles similar to those experienced in heat treatment practice. The structure of the steel will be changed in this region (called the heat affected zone, HAZ).

## Slide 11: Effect of the Welding Thermal Cycle on the Microstructure
The intense heat involved in the welding process influences the microstructure of both the weld metal and the parent metal close to the fusion boundary.
The molten weld pool is rapidly cooled which results in the weld metal having a rapid cooling cast microstructure.
The weld filler metal need not to have the same composition as the parent metal. If the compositions were the same, the rapid cooling could result in hard and brittle phases, e.g. martensite, in the weld metal microstructure. This problem is avoided by using weld filler metals with a lower carbon content than the parent steel.
The parent material close to the fusion boundary is heated into the austenite phase field. On cooling, this region transforms to a microstructure which is different from the rest of the parent material. In this region the cooling rate is usually rapid, and hence there is a tendency towards the formation of low temperature transformation structures, such as bainite and martensite, which are harder and more brittle than the bulk of the parent metal. This region is known as the heat affected zone (HAZ).

## Slide 12: The Heat Affected Zone (HAZ)
The microstructure of the HAZ is influenced by three factors:
-The chemical composition of the parent metal which determines the
hardenability of the HAZ.
-The heat input rate during welding which directly affects the grain size in
the HAZ. A high heat input rate leads to a longer thermal cycle and thus a
coarser HAZ microstructure. The higher the heat input rate the lower the
cooling rate. The value of heat input rate is a function of the welding
process parameters: arc voltage, arc current and welding speed.
-The cooling rate in the HAZ after welding which is also influenced by 2 other factors; (i) the joint design and thickness which determine the rate of heat flow away from the weld during cooling. (ii) the temperature of the parts being joined, i.e. any pre-heat, is significant since it determines the temperature gradient which exists between the weld and parent metal.

## Slide 13: Vulnerabilities of the Heat Affected Zone (HAZ)
If the workpiece material was previously cold worked, recrystallization and grain growth may occur in HAZ; reduce strength, hardness, and toughness.
Upon cooling, residual stresses may form in this region that weaken the joint.
The material in this zone may get heated to temperatures sufficiently high so as to form austenite. Upon cooling to room temperature, the microstructural products that form depend on cooling rate and alloy composition. For plain carbon steels, normally pearlite and a proeutectoid phase will be present. For alloy steels it is martensite.
Some stainless steels may be “sensitized” during welding, which renders them susceptible to intergranular corrosion.
Local melting can occur at grain boundaries (liquation cracking) due to the presence of constituents having a lower melting point than the surrounding matrix. Fine cracks may be produced in this region if the residual stress is high. These cracks can be extended by fabrication stresses or during service.
Hydrogen induced cracking due to presence of hydrogen (rapid cooling & residual).

## Slide 14: Residual Stresses and Distortion in Welding
The intense heat associated with welding causes the region of the weld to expand and contract on cooling. This is resisted by the surrounding cold material leading to a residual stress in the vicinity of the weld.
In the weld metal the residual stress tends to be mostly tensile in nature which is balanced by a compressive stress induced in the parent metal.
The residual stresses arise because the material undergoes local plastic strain which may result in cracking of the weld metal/HAZ during welding, distortion of the parts or susceptibility to brittle failure during service.
Transverse and longitudinal contractions in welding can lead to distortion if the hot weld metal is not symmetrical about the neutral axis of a fabrication.
Angular rotation can occur due to the major part of the weld being on one side of the neutral axis of the plate, thus inducing greater contraction stresses on that side. This leads to a distortion known as cusping.
Distortion problems can be avoided by correct weld preparation; use of non-symmetrical double-sided welds (balanced welding), welding should be started at the centre of a fabrication and all succeeding welds be made from the centre out, thus encouraging contractions to occur in the free condition.

## Slide 15: Residual Stress Relief
The most common and efficient way of relieving residual stresses is by heating. Raising the temperature results in a lower yield stress and allows creep to occur. Creep relieves the residual stresses through plastic deformation. Steel welded components are usually heated to a low red heat (600°C) during stress relieving treatments.
The heating and cooling rates during the thermal stress relief must be carefully controlled otherwise further residual stress may be set up.
Thermally stress relieving is limited both by the size of the ovens required and the possibility of a structure distorting under its own weight. Small ovens can be placed around the joints or by using electric heating elements.
Other methods of stress relief rely on thermal expansion providing mechanical forces capable of counteracting the original residual stresses. Can be applied in-situ but a precise knowledge of the location of the compressive residual stresses is vital, otherwise the level of residual stress may be increased rather than decreased.

## Slide 16: Weld Metal Solidification Cracking
Solidification of the molten weld pool occurs by the growth of crystals away from the fusion boundary and towards the centre of the weld pool, until eventually there is no remaining liquid. Thus, solute and impurity elements are pushed ahead of the growing interface. At the final stages of solidification the growing crystals interlock at the centre of the weld.
The high concentration of solute and impurity elements can then result in the production of a low freezing point liquid at the centre of the weld. This acts as a line of weakness and can cause cracking to occur under the influence of transverse shrinkage strains.
Impurity elements such as sulphur and phosphorus are particularly important in this type of cracking since they cause low melting point silicides and phosphides to be present in the weld metal.
Even with weld metals with low sulphur and phosphorous cracking may still arise in the following circumstances; (i) Joint movement occurs during welding, (ii) Contamination of the weld metal with elements such a sulphur and phosphorus, (iii) The weld metal has to bridge a large gap, (iv) the diffusion of impurity elements from the steel into the weld metal.

## Slide 17: Weldability of Steels
A structural steel is weldable if joints in the steel behave satisfactorily in service; the welded joint microstructure should have sufficient ductility to resist residual stresses, arising from the welding thermal cycle, without cracking.
Weldability, influenced by the chemical composition (CEV) and also by the metallographic structure of the steel. The CEV takes account of the important elements which affect hardenability. A typical formula for the CEV = (BS EN 10025 sets mandatory limits for CEV for all structural steel products).
Hardening in the HAZ can be avoided by using a steel with a CEV < 0,42.Increasing the content of alloying elements decrease weldability. Whereas grain refinement improves weldability.
The chemical compositions of both the weld and parent metals (CEV), together with the parameters of the welding process (heat input and cooling rates), are influential in determining joint ductility.
The level of impurity elements, such as S, P & H is a particularly significant factor in determining whether crack formation will occur during welding.

## Slide 18: Types of Weld Defects
Weld Technique defects - Stray arc and Spatter.
Weld Geometry defects - Weld profile (incorrect throat thickness, incorrect leg length, poor toe angle), Linear misalignment, Angular misalignment, Excess weld metal, Overlap, Incompletely filled groove, Undercut.
Cavities defects - Gas pores, Wormholes, Surface porosity, Crater pipes.
Cracks - Solidification cracks, Hydrogen induced cracks, Lamellar tearing.
Types of cracks: longitudinal cracks, transverse cracks, radiating cracks, crater cracks, branching cracks.
With the exception of crater cracks, that can only be found in the weld metal, all of the other types of crack can be situated; in the weld metal; in the HAZ; or in the parent metal.
Depending on their nature cracks can be; hot cracks (solidification cracks); precipitation induced cracks (reheat cracks); cold cracks (hydrogen induced cracks); lamellar tears.
Solid Inclusions - Slag inclusions, Flux inclusions, Oxide inclusions.
Lack of Fusion or Penetration - Lack of sidewall fusion, Lack of inter-run fusion, Lack of root fusion, Lack of penetration, Incomplete root penetration.

## Slide 19: Quality Criteria in Welding
BS EN 1090-2 requires welders to be qualified in accordance with BS EN ISO 9606-1. The standard prescribes tests to qualify welders based upon process, consumable, type of joint, welding position and material.
Welding procedures should be properly specified (Annex A of BS EN ISO 15609-1) to give a satisfactory welded joint. The major parameters are: welding position, electrode type, edge preparation, preheat, voltage, current, travel speed, number of runs and post-weld heat treatments.
Hot metal in the weld zone contracts during cooling causing residual stresses. Distortion will occur if appropriate control is not exercised.
It is necessary to support the WPS with evidence of satisfactory procedure tests in the form of a welding procedure qualification record (WPQR) prepared in accordance with BS EN ISO 15614-1.
By selecting an execution class in BS EN 1090-2, acceptance criteria are established, beyond which the imperfection is considered a defect.

## Slide 20
Inspection and testing of Welds
BS EN 1090-2 sets out the scope of inspection before, during and after welding and gives acceptance criteria related to execution class.
Non-destructive testing (NDT) methods is selected in accordance with EN 12062 by personnel qualified according to Level 3 as defined in EN 473. Generally UT or RT applies to butt welds & PT or MPT applies to fillet welds.
BS EN 12062 Non-destructive examination of welds — General rules for metallic materials refers to the following non-destructive examination (NDE) methods: Eddy current testing, Magnetic particle testing, Penetrant testing, Radiographic testing (X-ray), Ultrasonic testing, Visual testing.
It is not possible to use destructive testing on production weldments, but such methods are used in qualification testing of welders and welding procedures (EN ISO 15613). Some weld imperfections specified in BS EN ISO 5817 are difficult to characterise using NDT, and destructive tests are needed. The test methods possible in destructive testing are tensile tests, hardness tests, impact tests, bend tests, macroscopic & microscopic exam.

## Slide 21: Laser Beam welding
A relatively modern joining technique is that of laser beam welding, wherein a highly focused and intense laser beam is used as the heat source.
The laser beam melts the parent metal, and, upon solidification, a fusion joint is produced; often a filler material need not be used.
Some of the advantages of this technique are as follows: (i) it is a noncontact process, which eliminates mechanical distortion of the workpieces; (ii) it can be rapid and highly automated; (iii) energy input to the workpiece is low, and therefore the heat-affected zone size is minimal; (iv) welds may be small in size and very precise; (v) a large variety of metals and alloys may be joined using this technique; and (vi) porosity-free welds with strengths equal to or in excess of the base metal are possible.
Laser beam welding is used extensively in the automotive and electronic industries, where high quality and rapid welding rates are required.

## Slide 22: THANK YOU